## Slide 1: THOXAM THermal stability and Oxidation of highly Active Materials
D. Serrano Purroy, A. Milena Pérez
Kick-off meeting JRC-CIEMAT, Madrid, 4th March 2016

## Slide 2: THOXAM – THermal stability and Oxidation of highly Active Materials
2026 JRC/CIEMAT Call for Proposals
Duration: 4 years
Coordinators:
    D. Serrano Purroy (JRC) A. Milena Pérez (CIEMAT)
Core Scientific Team:
  Joint JRC-CIEMAT expertise in fuel degradation, Raman spectroscopy and high-temperature actinide behaviour
Main Objective:
  Establish a robust experimental framework to understand and predict thermal behaviour in corium and spent nuclear fuel

## Slide 3: THOXAM – Background & Strategic Evolution
Long-standing JRC-CIEMAT cooperation in nuclear fuel cycle safety
Since 2021: Joint work on Raman characterisation of SNF and secondary phases supported by mobility exchanges
  2021 - DISCO (Horizon 2020 mobility program): Raman characterisation of SNF samples and identification of secondary phases
  2022-23 - CIATFRAS (ActUslab): High temperature oxidation studies of SNF and ATF
Scientific Gap Identified
  Limited understanding of oxidation behavior of highly active corium materials and MOX
  Insufficient data on long-term structural evolution under thermal stress

## Slide 4: Scientific Foundations of THOXAM – Raman Characterisation of SNF
BU | 63 MWd/kgU
Temperature | 350 ºC
Heating rate | 50 ºC/min
Atmosphere | Air (80 mL/min)

## Slide 5: Scientific Foundations of THOXAM – High-Temperature Oxidation of SNF
Pellet centre
T=350 ºC
U3O8 detected after 62h
Homogeneous oxidation

## Slide 6: Scientific Foundations of THOXAM – High-Temperature Oxidation of HBS
Pellet rim
T=350 ºC
U3O8 detected after 92h
Heterogeneous oxidation
Oxidation delayed at the rim

## Slide 7: Scientific Foundations of THOXAM – ATF under Thermal Stress
 | Standard UO2 | Cr-doped UO2
Reactor type | PWR | PWR
BU | ~60 MWd/kgU | ~60 MWd/kgU
Grain size | - | ~60 µm
Cr content | - | ~0.2 wt.%
High-burnup standard UO2
High-burnup Cr-doped UO2 ATF
ATF sample tested at 400 ºC for extra 200 h and still finding U4O9 at both the centre and the rim
Greater oxidation resistance of the Cr-doped UO2 fuel (compared to undoped)
Greater oxidation resistance at the pellet rim (compared to the centre)
 Potential benefits of ATFs and high burnup
T=400 ºC
T=350 ºC

## Slide 8: Scientific Foundations of THOXAM – Knowledge gaps and Open Questions
Study corium thermal stability and phase evolution following the same protocol by Linkam-Raman
Characterize crystalline phases of corium to analyse their role as potential reservoirs of radionuclides present in SNF, avoiding its release
Comparison with (U,Zr)O2 reference samples, already fabricated and characterized at JRC (G.5)
2023-1-RD-ActUsLab-FMR, carried out by J.M. Elorrieta
TMI-2 Sample

## Slide 9: THOXAM - Objectives
Scientific Objectives
  Characterize oxidation-driven phase transformations in corium (TMI-2, Chernobyl)
  Quantify thermal stability and structural degradation mechanisms
  Extend methodology to SNF and MOX systems
  Generate experimental data supporting safety case development

## Slide 10: THOXAM - Milestones & Expected Deliverables
Milestones
Key Deliverables
Strategic Impact
Strengthens institutional integration and advances European radioactive waste management research
M1 – Harmonised protocol (M2)
M2 – Corium dataset (M24)
M3 – Comparative assessment (M36)
M4 – Consolidated framework (M48)
Joint JRC–CIEMAT oxidation database
High-impact peer-reviewed publications
Technical reports supporting disposal safety
Contribution to European safety assessment performance studies

## Slide 11: Thank you
HLWU
Notes: Update/add/delete parts of the copy right notice where appropriate.
More information: https://myintracomm.ec.europa.eu/corp/intellectual-property/Documents/2019_Reuse-guidelines%28CC-BY%29.pdf