## Slide 1
GRAFAGEN PROJECT
SYNTHESIS AND CHARACTERIZATION OF GRAPHENE-BASED MATERIALS FOR HYDROGEN STORAGE
Alberto J. Quejido - M. Isabel Rucandio - Rodolfo Fernández - M. Belén Gómez
Chemistry Division of CIEMAT

## Slide 2
Objectives
Introduction
Proposed Method
Further study
Capabilities
Outline

## Slide 3
1. Objectives of the GRAFAGEN project
Synthesis of a different graphene-based materials hydrothermal processing of Graphene Oxide, previously prepared by Hummers method, with transition metals salts followed by calcination.
Characterization of synthetized materials by different macro-, micro- and nanoestructural techniques.
Study of adsorption/absorption and desorption of hydrogen in the prepared materials-
1.1 Preparation of graphene supported in different material by CVD
1.2 Applications of graphene for PV applications
1.3 Synthesis of different graphene bases materials for H2 storage

## Slide 4
2. Introduction
Graphite(Gt)
Graphene
Mechanical exfoliation(adhesive tape technique),
Graphite(Gt)
Graphite oxide(GtO)
Graphene oxide(GO)
Oxidation
(Hummers method)
Exfoliation
(sonication, stirring)
Graphene oxide(GO)
Reduced graphene oxide(rGO)
Reduction (chemical reduction, thermal annealing)
2.1 Graphene-based materials

## Slide 5
2. Introduction
2.2 Graphene-based materials: Properties
Electrical
  Zero-overLap semimetal with both holes and electrons as charge carriers
  Very high electrical conductivity (depending on the quality of graphene)
Mechanical
    Young’s modulus ~ 1TPa
Optical
    Transmittance ~ 97,7%
Thermal
  Conductivity Above 3000 W.m.K-1
High Specific Surface Area
  Theoretically ~ 2620 m2.g-1

## Slide 6
2. Introduction
2.3 Metal Oxide-rGO nanocomposites by hydrogen storage
Graphite Oxide/Metal Salt
Metal Oxide-rGO
Hydrothermal
treatment
and Calcination
Metal Salt mixing with GO. Sonication
Oxidation
(Hummers
Method)
Graphite Powder
Graphite Oxide

## Slide 7
3. Proposed Method
Starting approach based on: “Effect of calcination temperatures on the electrochemical performances of nickel oxide/reduction graphene oxide (NiO/RGO) composites synthesized by hydrothermal method” Chen et al. (2016) Journal of Physics and Chemistryof Solids 98 209–219
  Easy implementation with our capabilities : Basic laboratory operations such as ultrasonic sonication, hydrothermal treatment, filtration, centrifugation…
  No highly sophisticated instrumentation is required.
  Cost-effective: minimum organic solvents consumption
Adaptation of ZnO and NiO proportions according to those from Z-Sorb III sorbent:
  ZnO 42,5% w/w and NiO 6,6% w/w are normalised to ZnO 86,5% w/w and NiO 13,5% w/w
3.1 Starting point conditions

## Slide 8
3. Proposed Method
3.2 Applied procedure
Graphite Powder (0,3g)
Hummers method
(KMnO4, H2SO4)
Graphite Oxide
Graphene Oxide
(GO)
Mechanical exfoliation
(Ultrasonication)
Graphite oxidation
Slow addition of
5.8 g Zn(NO 3)2
+ 0.9 g Ni(NO 3)2
+1 g Urea
Hydrothermal
treatment:
120 ˚C, 24h
Transfer to centrifuge tubes: Centrifugation Washing repeteadly with DI water and Ethanol
Drying under vacuum:
60 ˚C, 24h
Calcination:
250 ˚C, 24h
NiO/ZnO-rGO powder
Synthesis of composite
GO solution in DI water: 5 mg.L-1

## Slide 9
3. Proposed Method
3.3 Scheme of the device for H2 adsorption/desorption
H2
He for system purge
M1
Gas exhaust
Output for gas sampling and analysis (µGC)
Vacuum pump
Cylinder containing graphene sample
Stopper
Gas exhaust

## Slide 10
4. Further studies
Test GO obtained by improved Hummers method as starting material
  Increase the efficiency of graphite oxidation
Test different weight ratios among GO - Zn(NO3)2 - Ni(NO3)2
Test different calcination temperatures

## Slide 11
5. Capabilities of the Chemistry Division of CIEMAT
Chemical synthesis of different graphene-based materials (doping, structural modifications or prepared in different forms – powder, sheets, ribbons-).
Structural characterization and chemical purity.
To check electrical properties of prepared materials.
To build specifically designed devices for different applications.

## Slide 12
Thanks for your kind attention and we are ready for your questions or suggestions!!